

TECHNICAL SHEET

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
| **Designation** | **POWDER FREE LATEX EXAMINATION GLOVES SOFT** | | | | |
| **Reference** | XS -5/6 | S – 6/7 | M – 7/8 | L-8/9 | XL-9/10 |
| 3135786 | 3135787 | 3135788 | 3135789 | 3135790 |
| **Visual product** |  | | | | |
| **Product description** | * Powder-free latex examination gloves, chlorinated. * Non-sterile, with micro-textured surface and rolled cuffs. * Polymer coated | | | | |
| **Characteristics and composition** | |  |  |  |  |  |  | | --- | --- | --- | --- | --- | --- | |  | XS -5/6 | S – 6/7 | M – 7/8 | L-8/9 | XL-9/10 | | Width of the palm (mm) | 70-79 | 80-89 | 90-99 | 100-109 | 110-119 | | Thickness at the finger | 0.15 ± 0.02 (0.14 – 0.16) | | | | | | Thickness at the palm | 0.12 ± 0.02 (0.12 – 0.14) | | | | |  * Protein content: max 50 µg/dm². * Powder level: max 2 mg/dm². * In compliance with the standards: EN 455-1/2/3/4, EN 420, EN 374-1/2/4/5 | | | | |
| **Packaging** | Box included 100 gloves (± 2 gloves).  10 boxes per carton. | | | | |
| **Shelf life** | 5 years from the date of manufacture. | | | | |
| **Indication for use** |  | | | | |
| **Legal information** | Medical Device of class I under MDR 2017/745  Class III personal protective equipment under Regulation 2016/425  CE Marking | | | | |

Version 1.1

Update 15/11/2022 by RG