

TECHNICAL SHEET

|  |  |
| --- | --- |
| **Designation** | **POWDER FREE LATEX EXAMINATION GLOVES SOFT**  |
| **Reference** | XS -5/6 | S – 6/7 | M – 7/8 | L-8/9 | XL-9/10 |
| 3135786 | 3135787 | 3135788 | 3135789 | 3135790 |
| **Visual product** |  |
| **Product description** | * Powder-free latex examination gloves, chlorinated.
* Non-sterile, with micro-textured surface and rolled cuffs.
* Polymer coated
 |
| **Characteristics and composition** |

|  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | XS -5/6 | S – 6/7 | M – 7/8 | L-8/9 | XL-9/10 |
| Width of the palm (mm) | 70-79 | 80-89 | 90-99 | 100-109 | 110-119 |
| Thickness at the finger | 0.15 ± 0.02 (0.14 – 0.16) |
| Thickness at the palm | 0.12 ± 0.02 (0.12 – 0.14) |

* Protein content: max 50 µg/dm².
* Powder level: max 2 mg/dm².
* In compliance with the standards: EN 455-1/2/3/4, EN 420, EN 374-1/2/4/5
 |
| **Packaging** | Box included 100 gloves (± 2 gloves). 10 boxes per carton.  |
| **Shelf life** | 5 years from the date of manufacture.  |
| **Indication for use** |  |
| **Legal information** | Medical Device of class I under MDR 2017/745Class III personal protective equipment under Regulation 2016/425CE Marking |

Version 1.1

Update 15/11/2022 by RG