TECHNICAL SHEET

| Designation | Sterilisation pouches Medibase |  |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Reference(s) | SELF SEALING POUCHES |  |  |  |  |  |  |  |  |  |  |
|  | Size | 8,5 x 16,5cm |  | 7 x 25,5cm | 9 x 25,5cm | 14 x 28cm | 25,5 x 38cm | 5,7 x 13cm | 18 x 33cm | 9 x 13cm | 30 x 45 cm |
|  | Ref | 3135469 |  | 3135470 | 3135471 | 3135472 | 3135473 | 3135474 | 3135475 | 3135476 | 3135477 |
|  | HEAT SEALING POUCHES |  |  |  |  |  |  |  |  |  |  |
|  | Size | 7 x 25,5cm |  |  |  | 9 x 25,5cm |  |  | 20 x 33cm AVEC SOUFFLET DE 5,5cm |  |  |
|  | Ref | 3135479 |  |  |  | 3135480 |  |  | 3135478 |  |  |
| Product picture |  |  |  |  |  |  |  |  |  |  |  |
| Product description | Sterilization bags recommended for autoclaving or chemiclave. |  |  |  |  |  |  |  |  |  |  |
| Characteristics and composition | Paper |  | The basis paper weight is ±60g/m2, fitting the requirements of sterile packaging manufactured paper which list on ISO11607-1, 2 and EN868-5; According to the pouch designs, the printed inscription on the rolls is navy blue (Pantone298U), printing steam and EO indicator. |  |  |  |  |  |  |  |  |
|  | Film |  | Lucid wathet blue hyperthermal PET/CPP complex film, thickness is ±0,052mm, weight is 56 g/m2, conforming to the related requirements of EN868-5. |  |  |  |  |  |  |  |  |
|  | Ink |  | Using ink; the min printing area of indicator should be 100mm2, may not fade or become stained. |  |  |  |  |  |  |  |  |
| Packaging | Box of 200 pouches, available in 10 sizes |  |  |  |  |  |  |  |  |  |  |
| Shelf life | 5 years from manufacturing date |  |  |  |  |  |  |  |  |  |  |
| Indications of use |  |  |  |  |  |  |  |  |  |  |  |
| Legal information | Medical Device of class I CE Marking Manufacturer: FOMED Industries Inc |  |  |  |  |  |  |  |  |  |  |

Version 2.3						Updated 15/11/2022 by RG